**Henkel Chemical Spec Sheet for CC-157 offered by**:

**Line: “1”**

**Width: 66”**

**Speed: 300fpm Substrate: Aluminum**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| STAGE | 1 | 2 | 3 | 4 | 5 |
| PRODUCT | PCL 305R | WATER | K702SLK/AC | WATER | WATER |
| TANK VOLUME | 3400 GL | 1550 GL | 2000 GL | 1300 GL | 1300 GL |
| DWELL AT MAX SPEED | 20 SEC | 3 SEC. | 6 SEC. | 3 SEC. | 3 SEC |
| TANK CONSTRUCTION | CRS | CRS | CRS | CRS | CRS |
| HEATING | PLATE | PLATE | PLATE | *NIA* | PLATE |
| MAX TEMP | 120-130 F | 120-140F | 100-120F | AMB | 140 -150  MAX |
| PRESSURE | 40 PSI | 40 PSI | 40 PSI | 40 PSI | 40 PSI |
| LEVEL CONTROL | HENKEL | HENKEL | HENKEL | HENKEL | HENKEL |
| REPLESNISHING PUMPS | YES | NO | YES | NO | YES |
| AUTODRAIN | HEADER | NONE | HEADER | NONE | NONE |

TABLE OF CONTENTS

Section 1 Process Manual

|  |  |  |
| --- | --- | --- |
| Revision Date:  03/2006 | Stage  Stage 1 | Chemical Process  Parco Cleaner 305R |
| 02/16/04 | Stage 2 | Hot Water Rinse |
| 02/16/04 | Stage 3 | Bonderite K702SLK/AC |
| 02/16/04 | Stage 4 | Cold Water Rinse |
| *02116104* | Stage 5 | Hot Water Rinse |
| 01122/09 | Stage 1 | Parco Cleaner 305R |
| 01/22/09 | Stage 2 | Hot Water Rinse |
| 01/22/09 | Stage 3 | Bonderite |
|  |  | K702SLK/AC |
| *01122109* | Stage 4 | Cold Water Rinse |
| *01122109* | Stage 5 | Hot Water Rinse |